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Manganese Sulfate Mono CAS 10034-96-5
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Manganese Sulfate Mono CAS 10034-96-5is Used as a porcelain glaze, as a fertilizer additive and as a catalyst. It is added to soils to promote plant growth, especially of citrus crops. It is a good reducing agent for manufacturing paints, varnish driers. It is used in textile dyes, fungicides, medicines and ceramics. In foods, it is used as a nutrient and dietary supplement. It is also used in ore flotation, as a catalyst in viscose pro- cess and in synthetic manganese dioxide. In veterinary medicine, it is used as a nutritional factor and in the prevention of perosis in poultry.

EINECS No.:2 32-089-9

CAS No.: 10034-96-5

Apperance: pinkish powder or granular

H.S. Code: 2833.299090

31.8% min Manganese Sulphate powder

Detailed specification sheet

	ITEM
	UNIT
	SPECIFICATION

	Mn
	min
	31.8

	Pb
	max
	0.001%

	As
	max
	0.0005%

	Cd
	max
	0.001%

	Ni
	max
	100ppm

	Co
	max
	100ppm

	Fe
	max
	0.004%

	Cl
	max
	0.005%

	PH
	5.0-6.5
	5.5

	Water Insoluble
	max
	0.05%

	Fineness (pass 250 um sieve
	min
	95%


31.%min Manganese Sulphate granule
	ITEM
	UNIT
	SPECIFICATION

	Mn
	min
	31.5%

	Pb
	max
	0.001%

	As
	max
	0.0005%

	Cd
	max
	0.001%



Company Information
 

Xiamen Ditai Chemicals Co., Ltd is a professional chemical company in China.  We are proud our quality chemcials and service was approbated by the clients in the worldwide.
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Components: Guaranteed Analysis:  Typical Analysis:|  Methods:
Nanganese (in) : 31. Bmin >+32.01% HG/TI%ZB%Z’
Heavy Metal(hs Pb): 0.002% _max <0.001% HG_ 2936-1999
Iron (Fe): 0.004% max 0.002% HG/TI%ZB%Z
Vater Insoluble: 0.05% max 0.03% HG/TI%ZB%Z’
Cadmivn (0o : 0.001% _max < 0. 0005% [GB/T13082-1991
Arsenic(hs) : 0. 001%max <0. 0005% HG 2936-1999
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